## Slide 1: How inhomogeneities enhance the manipulability of Ge spin qubits
JOSÉ CARLOS ABADILLO-URIEL, BIEL MARTINEZ, ESTEBAN RODRIGUEZ, YANN-MICHEL NIQUET
CEA GRENOBLE
Now Comfuturo fellow at icmm-csic
Phys. Rev. B 106, 235426 (2022) | arXiv:2212.03691 (2022)

## Slide 2: outline
Introduction to semi & hole qubits
Usual manipulation of hole qubits
Inhomogeneous electric fields
Inhomogeneous strains
Conclusions

## Slide 3: Why semiconductor qubits?
Semiconductor Industrially compatible
Good coherence times & gate manipulability
Prospects of scalability (small unit cell)
Possible avenue for high-temperature operation (4K)
see, e.g. Nature 580, 355-359 (2020)
From Chatterjee et al., Nature Reviews Physics, 3, 157-177 (2021)

## Slide 4: Why hole spin qubits?
Qubit properties are highly tunable through gate voltages
Cool physics: anisotropic g-matrices, Rashba SOC, sweet spots
High SOC : fast all-electrical manipulation
    Hendrickx et al., Nature 591, 580–585 (2021)
  State of the art
  4-qubit processor: single-qubit gates above 99.9% and
  two-qubit above 99% (Hendrickx et al., Nature 591, 580–585 (2021))
  Large coherence T2*~90 μs (Piot et al., Nat. Nano (2022))
  “Hot”-qubit operation ~ 4K (Carmenzind et al., Nat. Electronics 5, 178–183 (2022))
  Spin-photon coupling of 330 MHz in hybrid Si-cQED system (Yu et al., Nature Nanotechnology (2023))

## Slide 5: Manipulating hole spins
-Hole spin is coupled to its motion
for holes in Ge, g_x ~ g_y ~ 0.15 g_z ~ 13.5
-Hamiltonian of a hole under a magnetic field
-We focus on planar dots (isotropic in-plane confinement)

## Slide 6: Rashba spin-orbit coupling
-Lack of inversion symmetry. Determined by geometry and gates
Michal et al., Phys. Rev. B 103, 045305 (2021)
Bosco et al., Phys. Rev. B 104, 115425 (2021)
-Nanowire or anisotropic dots (linear Rashba).
See Golovach et al. (2006) PRB 74
-Planar isotropic dots (cubic Rashba)
Only effective when magnetic field is vertical Bz
In the experiments the magnetic field is in-plane Bx

## Slide 7: g-tmr
-g-factor is anisotropic. By driving g-tensor the hole feels a time-dependent magnetic field
-Deforming the dot with electric fields induces changes in the g-tensor
Effective when
Crippa et al. (2018) PRL 120
Kato et al. (2003) Science 229
0.5
1
1.5
2
qxz
g(V(t))

## Slide 8
In the experiment, they use in-plane magnetic fields which are inefficient for both cubic Rashba and gTMR
Is there some missing mechanism?
Reviewing the usual assumptions:
-Separable and homogeneous confinement field
-Biaxial strains
Explaining hole experimental data

## Slide 9
INHOMOGENEOUS & NON-SEPARABLE CONFINEMENT FIELDS
Gates have finite size and are separated a certain distance away from the hole

## Slide 10
Non-separable field allows in-plane manipulation
x
y
z
Cubic Rashba
Non-separable feature
Still, Rabi frequencies are low. What’s missing?

## Slide 11
INHOMOGENEOUS STRAIn
Device is made with different materials with different expansion coefficients
Strain is assumed to be biaxial due to barrier & well lattice mismatch
Numerically minimizing the elastic energy density at low T, leads to inhomogeneities commensurate with the gate stack

## Slide 12
STRAIN INDUCES NEW GTMR AND RASHBA MECHANISMS
x
y
z
Linearized Rashba
Enhanced in-plane feature
Rabi frequencies now match the experiment

## Slide 13
STRAIN slightly improves quality factors
In-plane sweet spot
Out-of-plane quasi-sweet spot

## Slide 14
Conclusions
Ge hole spin qubits are a promising platform for quantum computation
Holes exhibit interesting physics, some of it still to be unveiled
We found that non-separable field and inhomogeneous strains lead to new manipulation mechanisms
Optimal operation with in-plane magnetic fields for fixed qubit frequency
Manipulability is improved by these mechanisms while coherence is mostly unaffected at sweet spots

## Slide 17: We can capture the physics with a non separable potential
The effective Hamiltonian for GS heavy-hole subspace can be obtained through Schrieffer-Wolff transformation. The subbands couple through
Physically, it is similar to a gTMR mechanism
When the potential is separable